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   常 州 科 益 化 工 有 限 公 司

  CHANGZHOU KOYE CHEMICAL CO.,LTD.

RM 1116, 1117 ECO BUSINESS PLAZA, 66, EAST GUANHE ROAD, CHANGZHOU, JIANGSU, CHINA


	PRODUCT DATA SHEET

HEDP

	Synonyms
	1-Hydroxyethylidene-1, 1- diphosphonic acid

	CAS Number
	2809-21-4

	Einecs Number
	220-552-8

	UN No.
	3261

	Molecular Formula
	C2H8N3O7P2

	Molecular weight
	206.02

	Structural Formula
	Industrial

	Product Grade
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	Description 

& Application
	A scale and synergistic corrosion inhibitor for iron rust and mineral scale from pipes of cooling circulation water units and boilers; Metal chelate agent for color fixing and bleaching in textile; Complexing agent for electron plate and scale cleaning agent for metals.



	Safety Protection
	Acidity, avoid contact with eye and skin, once contacted, flush with water.


	Specification
	Active content (as acid)% : ≥90.0% 

Phosphorous acid(as PO33-) %: ≤2.5

Phosphoric acid(as PO43-)%: ≤0.7

Chloride (as Cl-) %: ≤ 1.0

pH（1% solution）: ≤ 2.0

Iron，as Fe(ppm) : 35 max
Appearance：White crystalline powder



	Package 
	25kg/bag. Stored in cool and dry place. 

	Shelf Life
	1 year.
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