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   常 州 科 益 化 工 有 限 公 司

  CHANGZHOU KOYE CHEMICAL CO.,LTD.

RM 1116, 1117 ECO BUSINESS PLAZA, 66, EAST GUANHE ROAD, CHANGZHOU, JIANGSU, CHINA


	TECHNICAL DATE SHEET

Zinc Chloride

	Synonyms
	Zinc Chloride

	CAS Number
	7646-85-7

	Einecs Number
	231-592-0

	Molecular Formula
	ZnCl2

	Molecular weight
	136.29

	Structural Formula
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	Product Grade
	Industrial



	Description 

& Application
	It is mainly used in battery industry as raw material,

dehydratror and catalyst in synthesis industry and mordant, mercerizator, starch gum and preserving in dyeing industry.



	Specification
	Zinc Chloride content %≥
97.5
Hydrochloric soda content (as ZnO) %
2.2
Sulphates (as SO4)content%≤
0.01
Barium (Ba)content%≤
0.1
Ferrous(Fe)content%≤
0.001
Heavy Metals(as Pb)content%≤
0.001
Zinc Corrosion test
---


	Package 
	25kg/ 50kg P.P.vacuum bag 

50kg pasteborad bucker/galvanises drums from inside ect

	Shelf Life
	1 year.
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