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	PRODUCT DATA SHEET
PAA

	Synonyms
	Polyacrylic Acid

	CAS Number
	9003-01-4

	Einecs Number
	202-415-4

	Molecular Formula
	(C3H4 O2)n

	Structural Formula
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	Product Grade
	Industrial


	Description 
& Application
	PAA is innoxious and soluble in water, it can be used in situations of alkaline and high concentration without scale sediment. PAA can disperse the microcrystals or microsand of calcium carbonate, calcium phosphate and calcium sulfate. PAA is used as scale inhibitor and dispersant for circulating cool water system, papermaking, weave, dyeing, ceramic, painting, etc.PAA can be used as scale inhibitor and dispersant in circulating cool water systems in power plants, iron & steel factories, chemical fertilizer plants, refineries and air conditioning systems.


	Safety Protection
	have hormesis to eye and skin,but no acute toxicity


	Specification
	Solid content % : ≥30
Free Monomer %：≤0.5
pH（1% solution）: ≤ 3.0
Density(20℃) g/cm3 : ≥1.090
Appearance: slight yellow transparent liquid

	Note:40%,45%,50% Polyacrylic acid can be supplied on demands.


	Package 
	Normally In 25kg net Plastic Drum.Stored in cool and dry place. 


	Shelf Life
	1 year.
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