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   常 州 科 益 化 工 有 限 公 司

  CHANGZHOU KOYE CHEMICAL CO.,LTD.

RM 1116, 1117 ECO BUSINESS PLAZA, 66, EAST GUANHE ROAD, CHANGZHOU, JIANGSU, CHINA


	PRODUCT DATA SHEET

PBTC.NA4

	Synonyms
	Tetra sodium of 2-Phosphonobutane-1,2,4-tricarboxylic acid

	CAS Number
	40372-66-5

	Einecs Number
	

	UN No.
	

	Molecular Formula
	C7H7O9P·Na4  

	Molecular weight
	358

	Structural Formula
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	Product Grade
	Industrial



	Description 

& Application
	Widely used in circulating cooling water system and the oilfield water injection system of scale and corrosion inhibitor, especially suitable for use with zinc salt, copolymer, can be used for high temperature, high rigid, high alkali and need to run under high concentrated multiple occasions, as a chelating agent in the washing industry and metal cleaning agent. 

	Safety Protection
	

	Specification
	Active content（as acid）, %≥64
Active content（as salt）, %≥85
Total phosphorus(as PO43）, %≥22.5
Iron,(AS Fe2+),Mg/L ≤20
pH（1% solution）: 4.0-6.0
Appearance： White crystalline powder


	Package 
	25kg/bag.,Stored in cool and dry place.  


	Shelf Life
	1 year.
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