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	PRODUCT DATA SHEET

Polyquaternium-11 

	Synonyms
	Quaternized copolymer  of  vinylpyrrolidone  and dimethylaminoethyl methacrylate

	CAS Number
	53633-54-8

	Einecs Number
	611-022-0

	UN No.
	

	Molecular Formula
	C18H34N2O7S

	Molecular weight
	422.5368

	Structural Formula
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	Product Grade
	Industrial

	Description 

& Application
	As a macromolecule film-forming agent, it has characteristics of cation and superior styling and conditioning properties.
Mainly used in Mousses, Conditioners, Hair spray gels, Shampoos, Styling, Curl, Hair dyes products.

	Safety Protection
	

	Specification
	Appearance
colorless to light yellow viscous liquid
Solid(%)
20±1%
P.H(1% water solution 25℃)
4-6
Deficient
≤1.0%
Viscosity (CPS/25℃)
20000~70000


	Package 
	125kg/200kg net in plastic drum

	Shelf Life
	1year
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